11803 N Saguaro Blvd. Ste. 11   |   Fountain Hills, AZ 85268

SLAC-27

PRODUCT DESCRIPTION AND USE

SLAC-27 is a clear, solvent-based acrylic designed for sealing conventional concrete,

exposed aggregate, porous tile, concrete pavers, and a variety of architectural concrete surfaces.

SLAC-27  is based on a hard acrylic polymer that produces coatings that give good gloss, stain resistance,

and cleanability. Adhesion to properly prepared cementitious surfaces is excellent

and the material is completely non-yellowing. SLAC-27 is formulated to bring out the rich, natural beauty of the substrate.

Chemical Composition

High molecular weight thermoplastic acrylic resin dissolved in a specially formulated blend of

solvents.

Limitations

• Do not use on exterior on-grade flagstone, sandstone or slate.

• Use in heavy foot traffic areas requires regular maintenance coating.

• Use of any other product on top of SLAC-27 requires thorough mechanical abrading to insure

intercoat adhesion or the use of a Polyurethane 250 tie coat.

• Will not resist solvents or brake fluid.

• Concrete must be absolutely dry.

TECHNICAL DATA

Physical Properties

Solids Content, by Weight ............................................................................... 27%

Volatile Organic Compounds (Standard formula) ............................. 580 grams/liter

Volatile Organic Compounds (San Diego County and OTC States) 399 grams/liter

Volatile Organic Compounds (California formula) ............................ 100 grams/liter

Tukon Hardness ...................................................................................................16

60º Gloss (4 mil dry film) ......................................................................................75

Adhesion to Concrete (ASTM 451) ..................... concrete fails before loss of bond

Dry Times (77º6 mil wet film)

Recoat .................................................................................. 30-60 minutes

Light Traffic ..................................................................................... 4 hours

Full Cure ....................................................................................... 72 hours

Higher temperatures will shorten dry times and lower temperatures will lengthen dry times.

Thicker films will take longer to dry.  Thicker films may produce bubbles from solvent evaporation thru the film; we recommend thin film coatings to avoid this.

WARRANTY INFORMATION

Slide-Lok guarantees that this product is free from manufacturing defects and complies with our published specifications. In the event that the buyer proves that the goods received do not conform to these specifications or were defectively manufactured, the buyer’s remedies shall be limited to either the return of the goods and repayment of the purchase price or replacement of the defective material at the option of the seller. SLIDE-LOK CORPORATION  MAKES NO OTHER WARRANTY, EXPRESSED OR IMPLIED, AND ALL WARRANTIES OF MERCHANTABILITY AND FITNESS FOR A PARTICULAR PURPOSE ARE HEREBY DISCLAIMED. Slide-Lok Corporation shall not be liable for damages caused by application of its products over concrete with excessive moisture vapor transmission or alkalinity. Slide-Lok Corporation shall not be liable for any injury incurred in a slip and fall accident. Manufacturer or seller shall not be liable for prospective profits or consequential damages resulting from the use of this product.

GENERAL INFORMATION

- Moisture Vapor Emissions/Alkalinity Precautions:

All interior concrete floors not poured over an effective moisture vapor retarder are subject to

possible moisture vapor transmission and related high levels of alkalinity that may lead to

blistering and failure of the coating system. It is the coating applicator’s responsibility to conduct

calcium chloride and relative humidity probe testing to determine if excessive levels of vapor

emissions or alkalinity are present before applying any coatings.

- Surface Preparation:

Surface must be clean, sound and absolutely dry. Surface preparation should be done with a

floor machine and nylogrit type brush. Scrub the surface well using Slide-Lok's concrete cleaner and degreaser.  Do not let cleaning solution dry on the surface. Rinse well with water and allow to

dry overnight before coating.

- Application Recommendations:

SLAC-27 may be applied by brush, roller, airless sprayer or floor squeegee.  A 2 gallon “pump” bug sprayer found at the hardware store is an also effective means for applying the product.  If rolling the

material, use a 1/2-3/4 inch nap roller.  The same roller Slide-Lok recommends for use with its Polyaspartic coatings works well.  You may use a roller pan and use the dip and roll method. You may also pour “ribbons” of the product on the surface and roll out the material.  Because the material dries quickly when in a thin film,

apply liberal amounts, work small areas and keep a wet edge and work quickly.  Product will have a very long pot life but once rolled out, it will dry very quickly.  Distribute the material evenly by

slightly overlapping the area previously coated. Roll laterally across the body and roll again with

a vertical up and down motion. Application rates will vary from 200-400 sq. ft. per gallon

depending upon the texture and porosity of the substrate. SLAC-27 may be thinned with MEK,

Xylene or Acetone if desired. If using in California, use only Acetone to maintain VOC

compliance.

- Recoating:

SLAC-27 may be recoated with itself as soon as it is tack free, usually 20-40 minutes, depending on temperature. Recoating with itself after the material is fully cured requires that the surface be clean and dry.

No abrading is necessary. Recoating with other materials can be problematic and requires

thorough cleaning and abrading or the use of a Polyurethane 250 tie coat.  Always apply the non-SLAC-27 material to a small test area and conduct a tape pull test prior to the main application. Contact factory for specific test instructions. If using Polyurethane 250 tie coat, reduce the Polyurethane 250 50% with acetone. Apply one coat and allow to dry overnight before applying a second coat to avoid possible solvent attack.

- Handling Precautions:

Material is flammable. Extinguish all flames, pilot lights and electric motors until all vapors are

gone and the coating is hard. The vapor is harmful. Do not use indoors unless area can be

properly ventilated. Use a NIOSH approved cartridge type respirator during application. Avoid contact with skin, wear protective gloves. Read Material Safety Data Sheet before using.

- Slip and Fall Precautions:

OSHA and the American Disabilities Act (ADA) have now set enforceable standards for slip resistance

on pedestrian surfaces. The current coefficient of friction required by ADA is .6 on level surfaces and .8 on ramps. Slide-Lok recommends the use of angular slip resistant aggregate in all coatings or flooring systems that may be exposed to wet, oily or greasy conditions. It is the contractor and end users’ responsibility to provide a flooring system that meets current safety standards. Slide-Lok Inc. or its sales agents will not be responsible for injury incurred in a slip and fall accident.

Slide-Lok Inc.

PH: 480-222-9720   FX: 480-222-9711

11803 N. Saguaro Blvd Ste. 11   |   Fountain Hills, AZ 85268